Task Order 03 NDT Support

Deliverable 5.1.63 CC9 Baseline GPR Test Report

TABLE OF CONTENTS

Page

INTRODUCTION	1

TECHNICAL PRINCIPLE	1

FAA GPR SYSTEM	2

ANTENNA SELECTION	3

TESTING AND DATA COLLECTION	7

DATA ANALYSIS	12

DATA POST-PROCESSING	13

DETERMINATION OF GPR SIGNAL VELOCITY	18

LAYER THICKNESS DISTRIBUTION	21

900 MHz CART-MOUNTED ANTENNA	21

2 GHz VAN-MOUNTED ANTENNA	32

400 MHz VAN-MOUNTED ANTENNA	35

SUMMARY AND RECOMMENDATIONS	38

REFERENCES	39

APPENDIX A – DISTRIBUTION OF 2-WAY TRAVEL TIME (900 MHz ANTENNA)

APPENDIX B – DISTRIBUTION OF 2-WAY TRAVEL TIME (2 GHz ANTENNA)

APPENDIX C – DISTRIBUTION OF 2-WAY TRAVEL TIME (400 MHz ANTENNA)

APPENDIX D – DISTRIBUTION OF P-403MR/P-209MR/P-307MR THICKNESS (2 GHz ANTENNA)

LIST OF FIGURES

Figure	 Page

Figure 1. GPR image generation during a survey (Tarefder and Ahmed 2016).	1

Figure 2. GPR system: (a) cart-mounted, and (b) van-mounted.	2

Figure 3. Longitudinal profile of CC9 Pavement Test Section (GDIT 2020).	4

Figure 4. Instrumentation layout: (a) Plan view, and (b) Longitudinal profile of North (GDIT 2020)		5

Figure 5. GPR image of LFC-3N near instrumentations.	6

Figure 6. GPR image to distinguish thickness of P401MR: (a) 900 MHz, and (b) 2 GHz.	7

Figure 7. Survey layout for cart- and van-mounted GPR systems (GDIT 2020).	9

Figure 8. GPR survey: (a) cart-mounted system (N→S), and (b) van-mounted system (W→E).	10

Figure 9. GPR image: (a) Cart-mounted: 900 MHz, (b) Van-mounted: 400 MHz, and (c) Van-mounted: 2 GHz.	12

Figure 10. Post-processing of GPR image obtained from 900 MHz cart-mounted antenna.	14

Figure 11. 2-Way Travel Time from 900 MHz (LFS-1N): (a) P-401MR, and (b) P-403MR.	14

Figure 12. Post-processing of GPR image obtained from 2 GHz van-mounted antenna.	15

Figure 13. 2-Way Travel Time from 2 GHz (LFS-1N): (a) P-401MR, and (b) P-403MR.	16

Figure 14. Post-processing of GPR image obtained from 400 MHz van-mounted antenna.	17

Figure 15. 2-Way Travel Time in P-209MR (LFS-1N).	18

Figure 16. Metal plate calibration test.	19

Figure 17. P-401MR Thickness in LFS-1N/1S: (a) LFS-1N (STA: 0+15), (b) LFS-1S (STA: 0+15), (c) LFS-1N (STA: 0+30), and (d) LFS-1S (STA: 0+30).	22

Figure 18. P-401MR Thickness in LFS-2N/2S: (a) LFS-2N (STA: 0+75), (b) LFS-2S (STA: 0+75), (c) LFS-2N (STA: 0+90), and (d) LFS-2S (STA: 0+90).	23

Figure 19. P-401MR Thickness in LFC-3N/3S: (a) LFC-3N (STA: 1+35), (b) LFC-3S (STA: 1+35), (c) LFC-3N (STA: 1+50), and (d) LFC-3S (STA: 1+50).	24

Figure 20. P-401MR Thickness in LFS/LFC-4N/4S: (a) LFS-4N (STA: 1+95), (b) LFC-4S (STA: 1+95), (c) LFS-4N (STA: 2+10), and (d) LFC-4S (STA: 2+10).	25

Figure 21. P-401MR Thickness in LFC-5N/5S: (a) LFC-5N (STA: 2+55), (b) LFC-5S (STA: 2+55), (c) LFC-5N (STA: 2+70), and (d) LFC-5S (STA: 2+70).	26

Figure 22. P-403MR Thickness in LFS-1N/1S: (a) LFS-1N (STA: 0+15), (b) LFS-1S (STA: 0+15), (c) LFS-1N (STA: 0+30), and (d) LFS-1S (STA: 0+30).	27

Figure 23. P-403MR Thickness in LFS-2N/2S: (a) LFS-2N (STA: 0+75), (b) LFS-2S (STA: 0+75), (c) LFS-2N (STA: 0+90), and (d) LFS-2S (STA: 0+90).	28

Figure 24. P-209MR Thickness in LFC-3N/3S: (a) LFC-3N (STA: 1+35), (b) LFC-3S (STA: 1+35), (c) LFC-3N (STA: 1+50), and (d) LFC-3S (STA: 1+50).	29

Figure 25. P-307MR/P-209MR Thickness in LFS/LFC-4N/4S: (a) LFS-4N (STA: 1+95), (b) LFC-4S (STA: 1+95), (c) LFS-4N (STA: 2+10), and (d) LFC-4S (STA: 2+10).	30

Figure 26. P-209MR Thickness in LFC-5N/5S: (a) LFC-5N (STA: 2+55), (b) LFC-5S (STA: 2+55), (c) LFC-5N (STA: 2+70), and (d) LFC-5S (STA: 2+70).	31

Figure 27. P-401MR Thickness in LFS-1N/1S: (a) LFS-1N, and (b) LFS-1S.	32

Figure 28. P-401MR Thickness in LFS-2N/2S: (a) LFS-2N, and (b) LFS-2S.	33

Figure 29. P-401MR Thickness in LFC-3N/3S: (a) LFC-3N, and (b) LFC-3S.	33

Figure 30. P-401MR Thickness in LFS/LFC-4N/4S: (a) LFS-4N, and (b) LFC-4S.	34

Figure 31. P-401MR Thickness in LFC-5N/5S: (a) LFC-5N, and (b) LFC-5S.	34

Figure 32. P-401MR Thickness in LFS-1N/1S: (a) LFS-1N, and (b) LFS-1S.	35

Figure 33. P-401MR Thickness in LFS-2N/2S: (a) LFS-2N, and (b) LFS-2S.	36

Figure 34. P-154MR Thickness in LFC-3N/3S: (a) LFC-3N, and (b) LFC-3S.	36

Figure 35. P-154MR Thickness in LFS/LFC-4N/4S: (a) LFS-4N, and (b) LFC-4S.	37

Figure 36. P-154MR Thickness in LFC-5N/5S: (a) LFC-5N, and (b) LFC-5S.	37

LIST OF TABLES

Table	 Page

Table 1. CC9 Baseline GPR Testing (HEC 2020)	8

Table 2. Summary of P-401MR Thickness (900 MHz Antenna)	26

Table 3. Summary of P-403MR/P-209MR/P-307MR Thickness (900 MHz Antenna)	31

Table 4. Summary of P-401MR Thickness (2 GHz Antenna)	35

Table 5. Summary of P-209MR/P-154MR Thickness (400 MHz Antenna)	38

# INTRODUCTION

CC9 baseline Ground Penetrating Radar (GPR) testing was conducted using both cart-mounted and van-mounted systems between September 22 and 23, 2020 to:

- Determine pavement layer thicknesses

- Generate thickness profiles as the baseline to monitor thickness changes during the traffic test.

# TECHNICAL PRINCIPLE

GPR is an electromagnetic (EM) signal based nondestructive testing equipment for subsurface evaluation, that comprises a transmitter and a receiver (Saarenketo and Scullion 1999, Al-Qadi et al. 2003, and Ahmed et al. 2016). In Figure 1(a), the transmitter sends out a signal, which travels through air and then, pavement layers. The transmitted signal is reflected back to the receiver from the interfaces at varying depths. Later, amplitudes and 2-way travel times of the reflected signals corresponding to varying depths generate an amplitude vs. time plot, known as ‘A-scan’ (Figure 1(b)). In an ‘A-scan’, high positive amplitudes (i.e., A0, A1, and A2) are observed at the interfaces, whenever an EM signal travels through layers with dissimilar dielectric constants (ε), i.e., ε1 ≠ ε2. Note that dielectric constant in air (ε0) is 1.0, while it is 81 in water, and any geo-material (such as asphalt, aggregate, and soil) falls between these two thresholds (Cao et al. 2007). During a survey, all the A-scans recorded along the travel direction are stacked to generate an image of subsurface, known as ‘B-scan’ (Figure 1(c)).

(a)

(b)

(c)

Air (ε0 = 1)

Layer 1: h1, ε1

Layer 2: h2, ε2

Interface: 1

Interface: 2

Interface: 3

Figure 1. GPR image generation during a survey (Tarefder and Ahmed 2016).

# FAA GPR SYSTEM

The Federal Aviation Administration’s (FAA) GPR system includes a cart-mounted and a van-mounted Geophysical Survey Systems, Inc. (GSSI) GPR system, as shown in Figure 1(a) and (b). A 900 MHz ground-coupled antenna is placed in a plastic protective case within the cart-mounted GPR system, which is equipped with a Distance Measuring Instrument (DMI), and a 1-channel SIR 3000 controller (Figure 1(a)). The van-mounted GPR system comprises a 2 GHz air-coupled and a 400 MHz ground-coupled antenna, DMI, and 4-channel SIR 30 controller that communicates with 2 GHz and 400 MHz antennas simultaneously during testing. Both antennas are mounted in front of the van, while the DMI is attached to the left passenger wheel of the van. The entire data acquisition system, i.e., SIR 30 and monitor, resides inside the van.  Before CC9 baseline testing, all the components on both cart- and van-mounted GPR systems were ensured functional.

1-Channel SIR 3000 controller

DMI attached with a wheel

900 MHz antenna

(a)

2 GHz antenna

400 MHz antenna

(b)

Figure 2. GPR system: (a) cart-mounted, and (b) van-mounted.

# ANTENNA SELECTION

The initial plan was to conduct full-width GPR testing with cart-mounted 900 MHz antenna along transverse direction to monitor layer thickness changes due to permanent deformation under traffic loads and construct the cross-sectional layer profiles. To determine whether the 900 MHz antenna can capture all the pavement layers at both shallow and deeper depths, trial GPR testing was conducted using this antenna on CC9 test pavement. Figure 3 shows the longitudinal profiles of both north and south sides to demonstrate the as-built layer thicknesses distribution.

The 900 MHz antenna trial was conducted on north side over the instrumentation locations, i.e., Asphalt Strain Gage (ASG) and Pressure Cell (PC), to identify pavement layers, where the instrumentation served as ‘Ground-Truth’, i.e., buried object at a  known location and depth. Figure 4 shows the instrumentation layout, i.e., plan view and longitudinal profile of the north side. Figure 5 shows example images obtained from the trial over the ASG and PC locations, i.e., at offset: -17.25 and -15.00 feet respectively, on LFC-3N. Note that the horizontal axis stands for distance in feet, while the vertical axis stands for 2-way travel time in ns (nano-second). The top flat ‘Red Line’, i.e., positive amplitude as EM signal travels from one layer to the other with dissimilar dielectric constant, indicates the pavement surface, while the ‘Red Line(s)’ below indicate multiple layer interfaces underneath pavement surface. The image obtained from the ASG locations shows a ‘Red Line’ with four consecutive parabolas, which are considered as the ‘Ground-Truth’ for the bottom of P-401MR (Figure 5).

On the same figure, the GPR image over PC locations shows two parabolas at varying depths, where the top one aligned with the interface atop P-209MR and the bottom one was slightly below the interface atop P-154MR. On both images, some lifts of P-154MR were visible; however, layer interface atop P-152MR (subgrade) can only be barely identified. Similar observation was repeated during the identification of P-401MR, P-403MR, P-209MR, and P-307MR in LFS-1N through LFC-5N, while subgrade was not captured on the image in most cases.

As demonstrated in Figure 6, there was one more concern regarding the identification of thin P-401MR layer (as-built thickness of 3.3 inch) in LFC-5N. Even though the 900 MHz antenna identified P-401MR in all the test items during the trial, it was not able to capture the change in asphalt (P-401MR) thickness, in terms of 2-way travel time, between two consecutive test items, i.e., 5.1 inch in LFS-4N vs 3.3 inch in LFC-5N (Figure 6(a)). In a past study by Tarefder and Ahmed (2016), 2 GHz air-coupled antenna was used to identify thin asphalt sub-layer (approximately, 3.5 inch), while 400 MHz ground-coupled antenna was used to identify subgrade at the deeper depth (approximately, 25 inch). Therefore, additional trial testing was then conducted with the van-mounted GPR, where the thickness change in P-401MR between LFS-4N and LFC-5N was captured by the 2 GHz air-coupled antenna (Figure 6(b)). Layer interfaces at the deeper depths, i.e., wider range of 2-way travel time compared to that from 900 MHz antenna, were captured by 400 MHz antenna.

Finally, it was recommended to include the van-mounted GPR system with 2 GHz and 400 MHz antennas to CC9 baseline GPR testing so that both thin P-401MR including any bound/unbound material layers underneath, i.e., P-403MR, P-209MR, P-307MR, and P-154MR,  and subgrade at the deeper depth can be captured in the GPR image.

Figure 3. Longitudinal profile of CC9 Pavement Test Section (GDIT 2020).

(a)

(b)

Figure 4. Instrumentation layout: (a) Plan view, and (b) Longitudinal profile of North (GDIT 2020)

Pavement surface

ASGs at the bottom of P-401MR

PC atop P-209MR

PC atop P-154MR

LFC-3N (survey on ASG)

LFC-3N (survey on PC)

Note: ‘Red Line’ represents positive amplitude along interfaces between layers with dissimilar dielectric constants

Figure 5. GPR image of LFC-3N near instrumentations.

LFS-4N

LFC-5N

Pavement surface

Bottom of P-401MR

(a)

3.3-inch P-401MR in LFC-5N

5.1-inch P-401MR in LFS-4N

Note: ‘Red Line’ represents positive amplitude along interfaces between layers with dissimilar dielectric constants

(b)

Figure 6. GPR image to distinguish thickness of P401MR: (a) 900 MHz, and (b) 2 GHz.

# TESTING AND DATA COLLECTION

CC9 baseline GPR testing is summarized in Table 1. At the recommended stations, the full-width surveys were conducted with cart-mounted GPR system along the transverse direction (Figure 7). Prior to the full-width survey, cart-mounted GPR antenna was positioned along the ‘North Edge Marker’ as the ‘Start Point’, i.e., Offset: -26.66 feet, as shown in Figure 8(a). After positioning the antenna, the survey was conducted towards south direction and stopped once the antenna just crossed ‘South Edge Marker’, i.e., Offset: 26.66 feet.

Due to the sideway inaccessibility of the van-mounted GPR system to the test pavement, full-length survey was conducted at multiple offsets on both north and south sides, as shown in Figure 7. Note that there was approximately 4 feet of offset between the 2 GHz air-coupled and 400 MHz ground-coupled antenna. Prior to the full-length survey, the 2 GHz antenna of van-mounted GPR system was positioned at the ‘West End Marker’ as the ‘Start Point’, i.e., Station: 0 + 00, (Figure 8(b)), and then, the survey was conducted towards the east direction and stopped once the antenna crossed ‘East End Marker’, i.e., Station: 2 + 85.

During the survey, data collection parameter in the antenna controllers, i.e., SIR 3000 and SIR 30 for cart- and van- mounted GPR systems respectively, were set to: (a) Sampling rate: 512 samples/scan to capture the amplitude variation at the layer interface, (b) Scan per unit distance: minimum 12 scan/ft. to capture the continuity of layer thickness distribution as well as instrumentations such as ASGs, and (c) Gain: 1~3 point to ensure the visibility of the layer interfaces, for instance, bottom of P-401MR, P-403MR, P-209MR, P-307MR at shallow depth, and top of P-152MR at deeper depth. The data collection parameters can be set up according to the instructions in GSSI (2003) for SIR 3000 and GSSI (2011a) for SIR 30.

Table 1. CC9 Baseline GPR Testing (HEC 2020)

| Equipment | Antenna | Location |  |
| --- | --- | --- | --- |
|  |  | Transverse | Longitudinal |
| Cart-Mounted GPR | 900MHz ground-coupled | Full width (N→S)1 | STA 0+15, 0+30, STA 0+75, 0+90, STA 1+35, 1+50, STA 1+95, 2+10, STA 2+55, 2+70 |
| Van-Mounted GPR | 400MHz ground-coupled | OFF -17.25 feet, OFF -15.00 feet, OFF -12.75 feet, OFF +12.75 feet, OFF +15.00 feet, OFF +17.25 feet | Full length2 (W→E) |
| Van-Mounted GPR | 2GHz air-coupled | OFF -17.25 feet, OFF -15.00 feet, OFF -12.75 feet, OFF +12.75 feet, OFF +15.00 feet, OFF +17.25 feet | Full length (W→E) |

Note 1: From offset: -26.66 through +26.66 feet

Note 2: From station: 0 + 00 through 2 + 85

: Cart-mounted GPR

: Van-mounted GPR

17.25’

12.75’

-12.75’

-17.25’

Figure 7. Survey layout for cart- and van-mounted GPR systems (GDIT 2020).

Align the 900 MHz antenna along ‘North Edge’

(a)

Offset between two antennas: 4 feet

Align the 2 GHz antenna along ‘West End’

(b)

Figure 8. GPR survey: (a) cart-mounted system (N→S), and (b) van-mounted system (W→E).

Figure 9 shows example GPR images obtained from the baseline testing in the post-processing software RADAN 7, developed by GSSI (GSSI 2011b). Figure 9(a) shows an image obtained from a full-width survey with the 900 MHz cart-mounted antenna on LFS-1N. The top ‘Red Line’ (near 2-way travel time of 2.5 ns) represents the pavement surface whenever EM signal entered P-401MR from air and underneath surface, the ‘Red Line(s)’ at varying depths represent multiple layer interfaces, for instance, interface between P-401MR and P-403MR. Figure 9(b) shows an image obtained from the 400 MHz van-mounted GPR, the top ‘Red Line’ (corresponding to pavement surface) is aligned with the 2-way travel time of 0 ns, which was due to the automatic adjustment inside the software. In addition, the range of 2-way travel time for 400 MHz is 3-times the range for 900 MHz antenna, which ensures that 400 MHz antenna can identify deeper layers. Figure 9(c) shows the image from the 2 GHz air-coupled GPR antenna, where a ‘Green Line’ with negative polarity appears before the ‘Red Line’ that represents the ‘Direct Coupling’, i.e., EM signal from the transmitter directly reached the receiver after travels through air. It is only observed in the air-coupled antenna, due to the vertical offset (i.e., gap) between the bottom of antenna and pavement surface, as observed in Figure 5(b).

(a)

(b)

(c)

Figure 9. GPR image: (a) Cart-mounted: 900 MHz, (b) Van-mounted: 400 MHz, and (c) Van-mounted: 2 GHz.

# DATA ANALYSIS

To determine pavement layer thickness, the 2-way travel times (t) with high positive amplitude corresponding to the layer interfaces (As shown in Figure 1) were determined to interpret layer thickness using the following relationship (Tarefder and Ahmed 2016):

hi=viti-ti-12						(1)

where hi= thickness of i-th layer, vi= velocity of EM signal in i-th layer, ti= 2-way travel time at the bottom of i-th layer, , ti-1= 2-way travel time atop i-th layer, and i= 0, 1, 2…., while ‘0’ stands for pavement surface. Velocity of EM signal in a layer is as follows:

vi=cεi						(2)

where εi= dielectric constant of i-th layer, and c= speed of signal in air (= 11.8 in/ns or 0.3 m/ns) (Cao et al. 2007). Based on this formulation, pavement layer thicknesses were interpreted through: (a) Post-Processing of Baseline GPR Image to determine the 2-way travel time of EM signals in pavement layers, (b) Determination of EM signal velocity, and (c) Determination of layer thickness through Eq. (1).

## DATA POST-PROCESSING

GPR data files were first post-processed in RADAN 7 to track the layer interfaces and then, determine the ‘Total 2-Way Travel Time’ of EM signals reflected from multiple pavement layer interfaces (i.e., antenna transmitter sent out the signal towards pavement surface that traveled through pavement layers and portion(s) of it reflected back to antenna receiver from layer interfaces with dissimilar dielectric constants as discussed earlier).

900 MHz Cart-Mounted Antenna

Figure 10 shows a portion of the full-width GPR image captured by 900 MHz antenna on LFS-1N (STA: 0+15), where the survey distance of 0 feet was aligned with ‘North Edge Marker’, i.e., offset: -26.66 ft. The total 2-way travel times of EM signal corresponding to pavement surface, bottom of P-401MR, and P-403MR were determined from this image. This procedure was followed to post-process the remaining GPR images obtained from 900 MHz antenna. Note that some locations were discarded due to discontinuity in layer interface and/or poor image quality, which might be resulted from the noise from embedded instrumentation and/or conduit.

After tracking pavement surface followed by extraction of total 2-way travel time at pavement surface, bottom of P-401MR, and P-403MR on GPR image (Figure 10), 2-way travel time inside P-401MR and P-403MR, i.e., tP-401MR and tP-403MR respectively, were determined as follows:

tP-401MR=t1-t0						(3)

tP-403MR=t2-t1						(4)

tP-209MR=t2-t1						(5)

where t0= total 2-way travel time of signal reflected from pavement surface, t1= total 2-way travel time of signal reflected from the layer interface at P-401MR bottom, and t2= total 2-way travel time of signal reflected from the layer interface at P-403MR bottom. Note that t2 stands for total 2-way travel time of signal reflected from the layer interface at the bottom of P-209MR for LFC-3 through LFC-5 and P-307MR for LFS-4N.

Figure 11(a) and (b) show an example distribution of 2-way travel time within P-401MR and P-403MR respectively for LFS-1N. It is observed that 2-way travel time in P-401MR was shorter than that compared to P-403MR, indicating that the signal velocity in P-403MR was relatively smaller. Comparing the distribution between P-401MR vs P-403MR (Figure 11(a) and (b)), 2-way travel time in P-401MR was more consistent. In Figure 11(b), a drop in 2-way travel time in P-403MR was observed near Offset: 0 ft., which was in agreement with the as-built thickness distribution in LFS-1N and LFS-1S. The distributions of 2-way travel inside P-401MR and P-403MR for the remaining test items are included in APPENDIX A.

Pavement surface

Bottom of P-401MR

Bottom of P-403MR

Survey Distance, feet

Total 2-Way Travel Time, ns

tP-401MR

tP-403MR

t2

t1

t0

Figure 10. Post-processing of GPR image obtained from 900 MHz cart-mounted antenna.

(a)							(b)

Figure 11. 2-Way Travel Time from 900 MHz (LFS-1N): (a) P-401MR, and (b) P-403MR.

2 GHz Van-Mounted Antenna

Figure 12 shows a portion of the full-length GPR image (i.e., over LFS-1N + Transition area) captured by 2 GHz antenna, where the antenna was positioned at STA: 0 + 00 and Offset: -17.25 feet. Even though this antenna was intended to track P-401MR, layer interface along the bottom of the base layer, i.e., P-403MR in LFS-1N, was also captured in the image. Therefore, total 2-way travel time of signal reflected from pavement surface, bottom of P-401MR, and P-403MR were determined after tracking those layer interfaces. According to Eq. (3) and (4), 2-way travel time(s) of signal inside P-401MR and P-403MR were determined from the total 2-way travel time(s) along the layer interfaces, i.e., pavement surface, bottom of P-401MR and P-403MR.

Figure 13(a) and (b) show example distributions of 2-way travel time inside P-401MR and P-403MR respectively. Like 900 MHz antenna, 2-way travel time in P-401MR was shorter compared to that in P-403MR. In addition, the distribution for P-401MR was consistent. Note that some locations were discarded due to discontinuity in layer interface and/or poor image quality resulted from the noise caused by embedded instrumentation and/or conduit. The remaining 2-way travel time distributions for P-401MR and the base layers, i.e., P-209MR for LFC-3 through LFC-5 and P-307MR for LFS-4N, are included in APPENDX B respectively.

Survey Distance, feet

Total 2-Way Travel Time, ns

Pavement surface

Bottom of P-401MR

Bottom of P-403MR

tP-401MR

tP-403MR

t0

t1

t2

Figure 12. Post-processing of GPR image obtained from 2 GHz van-mounted antenna.

(a)							(b)

Figure 13. 2-Way Travel Time from 2 GHz (LFS-1N): (a) P-401MR, and (b) P-403MR.

400 MHz Van-Mounted Antenna

Figure 14(a) shows the GPR image captured by 400 MHz ground-coupled antenna during the full-length survey on LFS-1N at Offset: -15.00 feet. Since there was 4 feet offset between 2 GHz air-coupled and 400 MHz ground-coupled antenna  and 2 GHz antenna was set on STA: 0 + 00 prior to the full-length survey (Figure 8), survey distance of 4 feet on this GPR image represents STA: 0 + 00. Unlike image from 900 MHz antenna (Figure 10), pavement surface was automatically adjusted to total 2-way travel time of 0 ns on the image obtained by 400 MHz antenna, which eliminated the necessity of tracking pavement surface.

It was evident that 400 MHz can capture multiple layer interfaces at the deeper depths compared to 900 MHz antenna. On this image, the pressure cell atop P-152 MR (subgrade), i.e., STA: 0 + 00 as observed in Figure 4, serves as a ‘Ground Truth’ during tracking the layer interface atop P-152MR. Note that a higher gain point was used during the post-processing in RADAN 7 to enhance the visibility of the location of pressure cell for the demonstration of ‘Ground Truth’.

The layer interface atop P-152MR was tracked on full-length GPR survey images captured at the pre-selected offsets on both north and south sides, and an example image with tracked layer interface (at Offset: -17.25 feet) is shown in Figure 14(b). Total 2-way travel time of signal reflected atop P-152MR was determined and then the thickness of P-154MR:

tP-209MR=tP-152MR-t2						(6)

tP-154MR=tP-152MR-t2						(7)

where t0= total 2-way travel time of signal reflected from pavement surface, t1= total 2-way travel time of signal reflected from the layer interface at P-401MR bottom, and t2= total 2-way travel time of signal reflected from the layer interface at P-403MR bottom, which was obtained during the post-processing of 2 GHz antenna data.

Figure 14(b) shows an example distribution of 2-way travel time in P-209MR for LFS-1N. As mentioned earlier, some locations were discarded due to discontinuity in layer interface and/or poor image quality resulted from noise. Overall, the distribution was consistent.

Total 2-Way Travel Time, ns

Survey Distance, feet

Offset between 2GHz and 400 MHz antenna

Antenna at STA: 0 + 00

Pressure Cell atop P-152MR (STA: 0 + 22.5)

(a)

Interface atop P-152MR (subgrade)

LFS-1N (STA: 0+00 ~ STA: 0+45)

Offset between 2GHz and 400 MHz antenna

Total 2-Way Travel Time, ns

Survey Distance, feet

tP-152MR

(b)

Figure 14. Post-processing of GPR image obtained from 400 MHz van-mounted antenna.

Figure 15. 2-Way Travel Time in P-209MR (LFS-1N).

## DETERMINATION OF GPR SIGNAL VELOCITY

Velocity of GPR EM signal was determined based on: (a) ‘Ground Truth’ information for 400 and 900 MHz ground-coupled antenna, and (b) ‘Metal Plate Calibration Test’ for 2 GHz air-coupled antenna.

900 MHz Cart-Mounted Antenna

In Figure 5, instrumentations, such as ASG and PC, were identified in the GPR image captured by 900 MHz antenna, which served as the ‘Ground Truth’ of layer interfaces. During the post-processing, 2-way travel of signal inside the layers at this ‘Ground Truth’ were extracted and the signal velocity was determined as follows:

vP-401MR=2hP-401MRtP-401MR 					(8)

vP-403MR=2hP-403MRtP-403MR 					(9)

vP-209MR=2hP-209MRtP-209MR 					(10)

vP-307MR=2hP-307MRtP-307MR 					(11)

where vP-401MR, vP-403MR, vP-209MR, vP-307MR= signal velocities in P-401MR, P-403MR, P-209MR, and P-307MR respectively; hP-401MR, hP-403MR, hP-209MR, hP-307MR= as-built thicknesses of P-401MR, P-403MR, P-209MR, and P-307MR respectively at ‘Ground Truth’ locations; and tP-401MR, tP-403MR,tP-209MR, tP-307MR= 2-way travel times inside P-401MR, P-403MR, P-209MR, and P-307MR respectively at ‘Ground Truth’ locations. After the computation, ranges of signal velocity were: (a) P-401MR: 6.2~6.4, (b) P-403MR: 3.9, (c) P-209MR: 3.8, and (d) P-307MR: 3.5.

2 GHz Van-Mounted Antenna

Figure 16(a) demonstrate the ‘Metal Plate Calibration Test’, so-called ‘Bumper-Jump’ test, where 2 GHz air-coupled antenna was first placed above the metal plate (5-ft by 3-ft) with smooth and clean surface that ensures sufficient reflection of EM signals. Then, SIR 30 was activated to collect the data in ‘Time Scan Mode’. While the data was being collected, bumper of the van was bounced up and down several times to capture amplitudes of signals reflected back from the metal plate at the varying vertical offset between the antenna and metal plate. Figure 16(b) shows a portion of the GPR image captured during the bouncing up and down of the bumper. In RADAN 7, the calibration image was generated based on stacking the scans corresponding to the minimum towards the maximum vertical offsets. This calibration image (or file) was later integrated to a regular survey file to determine the signal velocities in pavement layers.

(a)

GPR Image in ‘Time Scan Mode’

Calibration Image

Total 2-Way Travel Time, ns

Scan Number

RADAN 7

(b)

Figure 16. Metal plate calibration test.

Once the calibration data file was integrated into the regular GPR survey file, dielectric constants (ε) of pavement layers were determined according to the following relationships (Edward and Mason 2011):

ε1=ε01+A0Am1-A0Am2						(12)

ε2=ε11+A1Am-A0Am21-A1Am-A0Am22					(13)

where ε0= dielectric constant of air (= 1.0); ε1= dielectric constant of P-401MR; ε2=  dielectric constant of P-403MR (for LFS-1 through LFS-2), P-209MR (for LFC-3 through LFC-5), and P-307MR for LFS-4N; A0,A1= amplitudes of signals reflected from pavement surface and bottom of P-401MR respectively; and Am= amplitude of signal reflected from surface of metal plate during the ‘Metal Plate Calibration Test’. The dielectric constants were then input into the following equations to determine the signal velocities:

v1=cε1						(14)

v2=cε2						(15)

where v1= signal velocity in P-401MR (=vP-401MR); v2= signal velocity in P-403MR (for LFS-1 through LFS-2), P-209MR (for LFC-3 through LFC-5), and P-307MR for LFS-4N (=vP-403MR, vP-209MR or vP-307MR); and c=  signal velocity in air (= 11.8 in/ns). Note that the entire set of formulations are embedded in RADAN 7 and it determines the signal velocities once a regular GPR data file and a calibration file is linked in the software. Later, a full-length baseline GPR survey file was linked to the calibration file generated from the ‘Metal Plate Calibration Test’ during the prep-work to determine the signal velocities in P-401MR, P-403MR, P-209MR, and P-307MR. Ranges of signal velocity were: (a) P-401MR: 4.6~4.8, (b) P-403MR: 4.4~4.5, (c) P-209MR: 4.3~4.5, and (d) P-307MR: 5.0.

400 MHz Van-Mounted Antenna

Like 900 MHz antenna, the ‘Ground Truth’ based approach was adopted to determine the signal velocities in the subbase, such as P-209MR in LFS-1 through LFS-2 and P-154MR in LFC-3 through LFC-5. During post-processing, 2-way travel of signal inside the subbase at the ‘Ground Truth’ (i.e., pressure cell atop P-152MR) were extracted and the signal velocity was determined as follows:

v3=2h3t3 						(16)

where v3= signal velocity in P-209MR or P-154MR;  h3= as-built thicknesses of P-209MR or P-154MR at ‘Ground Truth’ locations; and t3= 2-way travel times inside P-209MR or P-154MR at ‘Ground Truth’ locations. After the computations, ranges of signal velocity were: (a) P-154MR: 4.1~4.4, and (b) P-209MR: 4.1~4.2.

# LAYER THICKNESS DISTRIBUTION

After the determination of 2-way travel time(s) and signal velocities of pavement layers, layer thickness was calculated using Eq. (1). The distribution of GPR interpreted layer thicknesses are discussed in the following sub-sections:

## 900 MHz CART-MOUNTED ANTENNA

P-401MR Thickness

Figure 17(a) and (b) show the transverse profiles of P-401MR thickness in LFS-1N and -1S at STA: 0+15 respectively, while the similar profiles at STA: 0+30 are shown in Figure 17(c) and (d) respectively. At both stations, the transverse profiles showed consistent thickness distribution, except for a few locations where discontinuity was observed during tracking the layer interfaces due to noisy images. For LFS-1N and -1S, the mean P-401MR thicknesses were 5.0 and 4.9 inches with COV (%) of 2.8 and 2.7 respectively (as reported in Table 2). In both test items, GPR interpreted thicknesses were slightly greater than the as-built thickness, i.e., 4.9 and 4.4-inch thick P-401MR for LFS-1N and -1S respectively.

(a)							(b)

(c)							(d)

Figure 17. P-401MR Thickness in LFS-1N/1S: (a) LFS-1N (STA: 0+15), (b) LFS-1S (STA: 0+15), (c) LFS-1N (STA: 0+30), and (d) LFS-1S (STA: 0+30).

Figure 18(a) and (b) show the transverse profiles of P-401MR thickness in LFS-2N and -2S at STA: 0+75 respectively, while the similar profiles at STA: 0+90 are shown in Figure 18(c) and (d) respectively. For LFS-2N and -2S, the mean P-401MR thicknesses were 5.0 and 4.9 inches with COV (%) of 3.3 and 3.1 respectively (as reported in Table 2). Similar to LFS-1N and -1S, again GPR interpreted P-401MR thicknesses were slightly greater than the as-built thickness, i.e., 4.4-inch thick P-401MR for both LFS-2N and -2S.

(a)							(b)

(c)							(d)

Figure 18. P-401MR Thickness in LFS-2N/2S: (a) LFS-2N (STA: 0+75), (b) LFS-2S (STA: 0+75), (c) LFS-2N (STA: 0+90), and (d) LFS-2S (STA: 0+90).

Figure 19(a) and (b) show the transverse profiles of P-401MR thickness in LFS-3N and -3S at STA: 1+35 respectively, while Figure 19(c) and (d) show the similar profiles at STA: 1+50. For LFS-3N and -3S, the mean P-401MR thicknesses were 6.5 and 6.6 inches with COV (%) of 7.5 and 5.6 respectively (as reported in Table 2). Unlike LFS-1 and LFS-2 (both north and south), distributions of thickness were inconsistent. LFS3N and -3S comprise less stiff P-209MR in subbase layer with irregular surface, as compared to P-403MR base layer in LFS-1 and -2. It is speculated that aggregates of P-401MR pushed and possibly penetrated into the P-209MR base layer and then caused non-uniformly during the compaction, which led to inconsistent as-built layer interface between P-401MR and P-209MR and consequently, the interpreted layer thickness distributions were inconsistent. It was also observed that GPR interpreted P-401MR thicknesses were greater than the as-built thickness, i.e., 5.1 and 5.2-inch thick P-401MR for both LFS-3N and -3S.

(a)							(b)

(c)							(d)

Figure 19. P-401MR Thickness in LFC-3N/3S: (a) LFC-3N (STA: 1+35), (b) LFC-3S (STA: 1+35), (c) LFC-3N (STA: 1+50), and (d) LFC-3S (STA: 1+50).

Figure 20(a) and (b) show the transverse profiles of P-401MR thickness in LFS-4N and LFC-4S at STA: 1+95 respectively, and the similar profiles at STA: 2+10 are shown in Figure 20(c) and (d) respectively. Comparing LFS-4N and LFC-4S, thickness distributions in LFS-4N that was built on P-307MR were relatively consistent, since P-307MR was believed to be stiffer than P-209MR. The mean P-401MR thicknesses were 6.4 and 6.9 inches in LFS-4N and LFC-4S respectively, which were greater than the as-built P-401MR thickness (as reported in Table 2).

(a)							(b)

(c)							(d)

Figure 20. P-401MR Thickness in LFS/LFC-4N/4S: (a) LFS-4N (STA: 1+95), (b) LFC-4S (STA: 1+95), (c) LFS-4N (STA: 2+10), and (d) LFC-4S (STA: 2+10).

Figure 21(a) and (b) show the transverse profiles of P-401MR thickness in LFC-5N and -5S at STA: 2+55 respectively, while the similar profiles at STA: 2+70 are shown in Figure 21(c) and (d) respectively. For LFC-5N and -5S, the mean P-401MR thicknesses were 5.0 and 5.1 inches with COV (%) of 2.7 and 2.8 respectively (as reported in Table 2), while as-built thicknesses were 3.3-inch for both test items. Similar to the trial GPR testing, variation of layer interface at the bottom of thin P-401MR was not captured accurately by 900 MHz antenna, which explains the greater interpreted thickness and also, surprisingly high degree of consistency in case of P-401MR atop P-209MR base layer.

(a)							(b)

(c)							(d)

Figure 21. P-401MR Thickness in LFC-5N/5S: (a) LFC-5N (STA: 2+55), (b) LFC-5S (STA: 2+55), (c) LFC-5N (STA: 2+70), and (d) LFC-5S (STA: 2+70).

Table 2. Summary of P-401MR Thickness (900 MHz Antenna)

| Test Item | Start Station | End Station | As-built Thickness, inch | Interpreted Thickness, inch |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | Mean | COV (%) |
| LFS-1N | 0+00 | 0+45 | 4.9 | 5.0 | 2.8 |
| LFS-1S | 0+00 | 0+45 | 4.4 | 4.9 | 2.7 |
| LFS-2N | 0+60 | 1+05 | 4.4 | 5.0 | 3.3 |
| LFS-2S | 0+60 | 1+05 | 4.4 | 4.9 | 3.1 |
| LFC-3N | 1+20 | 1+65 | 5.1 | 6.5 | 7.5 |
| LFC-3S | 1+20 | 1+65 | 5.2 | 6.6 | 5.6 |
| LFS-4N | 1+80 | 2+25 | 5.1 | 6.4 | 3.3 |
| LFC-4S | 1+80 | 2+25 | 5.2 | 6.9 | 4.5 |
| LFC-5N | 2+40 | 2+85 | 3.3 | 5.0 | 2.7 |
| LFC-5S | 2+40 | 2+85 | 3.3 | 5.1 | 2.8 |

P-403MR/P-209MR/P-307MR Thickness

Figure 22(a) and (b) show the transverse profiles of P-403MR thickness in LFS-1N and -1S at STA: 0+15 respectively, while the similar profiles at STA: 0+30 are shown in Figure 22(c) and (d) respectively. Thickness drop was observed near the centerline, i.e., near offset: 0 feet, which was in agreement with the as-built thickness distribution of these test items. For LFS-1N and -1S, the mean P-403MR thicknesses were 5.8 and 4.3 inches with COV (%) of 4.8 and 5.5 respectively (as reported in Table 3). The interpreted P-403MR thicknesses were close to the as-built thicknesses, i.e., as-built thicknesses of 5.9 and 4.5 inch for LFS-1N and -1S respectively.

(a)							(b)

(c)							(d)

Figure 22. P-403MR Thickness in LFS-1N/1S: (a) LFS-1N (STA: 0+15), (b) LFS-1S (STA: 0+15), (c) LFS-1N (STA: 0+30), and (d) LFS-1S (STA: 0+30).

Figure 23(a) and (b) show the transverse profiles of P-403MR thickness in LFS-2N and -2S at STA: 0+75 respectively, while the similar profiles at STA: 0+90 are shown in Figure 23(c) and (d) respectively. Like LFS-1N and -1S, thickness drop was also observed on these test items near the centerline that reflects the as-built P-403MR thickness distribution. The mean P-403MR thicknesses were 5.8 and 4.2 inches with COV (%) of 6.9 and 8.7 for LFS-2N and -2S respectively (as reported in Table 3). As-built P-403MR thicknesses were 6.4 and 4.3 inches for LFS-2N and -2S respectively, which demonstrated a close match for LFS-2S; however, a difference for LFS-2N.

(a)							(b)

(c)							(d)

Figure 23. P-403MR Thickness in LFS-2N/2S: (a) LFS-2N (STA: 0+75), (b) LFS-2S (STA: 0+75), (c) LFS-2N (STA: 0+90), and (d) LFS-2S (STA: 0+90).

Figure 24(a) and (b) show the transverse profiles of P-209MR thickness in LFS-3N and -3S at STA: 1+35 respectively, while Figure 24(c) and (d) show the similar profiles at STA: 1+50. As mentioned earlier, several locations were discarded (data gap in the figures) from the thickness interpretation due to discontinuity in layer interface and/or poor image quality resulted from noise caused by the embedded instrumentation and/or conduit. The mean P-209MR thicknesses were 7.1 and 6.9 inches with COV (%) of 4.9 and 4.4 for LFS-3N and -3S respectively (as reported in Table 3). The as-built P-209MR thicknesses were 7.7 inches for LFS-3N and -3S, which were greater than the interpreted thickness.

(a)							(b)

(c)							(d)

Figure 24. P-209MR Thickness in LFC-3N/3S: (a) LFC-3N (STA: 1+35), (b) LFC-3S (STA: 1+35), (c) LFC-3N (STA: 1+50), and (d) LFC-3S (STA: 1+50).

Figure 25(a) and (c) show the transverse profiles of P-307MR thickness in LFS-4N at STA: 1+95 and STA: 2+10 respectively, while the similar profiles of P-209MR at STA: 1+95 and STA: 2+10 are shown in Figure 25(b) and (d) respectively. The mean thicknesses were 5.5 and 6.9 inches with COV (%) of 5.4 and 6.0 for LFS-4N and LFS-4S respectively (as reported in Table 3). The interpreted P-307MR thicknesses were 2.3 inch smaller than the as-built thickness, i.e., 7.8 inch.

(a)							(b)

(c)							(d)

Figure 25. P-307MR/P-209MR Thickness in LFS/LFC-4N/4S: (a) LFS-4N (STA: 1+95), (b) LFC-4S (STA: 1+95), (c) LFS-4N (STA: 2+10), and (d) LFC-4S (STA: 2+10).

Figure 26(a) and (b) show the transverse profiles of P-209MR thickness in LFC-5N and -5S at STA: 2+55 respectively, while the similar profiles at STA: 2+70 are shown in Figure 26(c) and (d) respectively. The thickness distributions were relatively consistent. The mean thicknesses were 4.7 inches for both test items, while the as-built thicknesses were 6.0 and 6.1 inches for LFC-5N and -5S respectively.

(a)							(b)

(c)							(d)

Figure 26. P-209MR Thickness in LFC-5N/5S: (a) LFC-5N (STA: 2+55), (b) LFC-5S (STA: 2+55), (c) LFC-5N (STA: 2+70), and (d) LFC-5S (STA: 2+70).

Table 3. Summary of P-403MR/P-209MR/P-307MR Thickness (900 MHz Antenna)

| Test Item | Start Station | End Station | Layer | As-built Thickness, inch | Interpreted Thickness, inch |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Mean | COV (%) |
| LFS-1N | 0+00 | 0+45 | P-403MR | 5.9 | 5.8 | 4.8 |
| LFS-1S | 0+00 | 0+45 | P-403MR | 4.5 | 4.3 | 5.5 |
| LFS-2N | 0+60 | 1+05 | P-403MR | 6.4 | 5.8 | 6.9 |
| LFS-2S | 0+60 | 1+05 | P-403MR | 4.3 | 4.2 | 8.7 |
| LFC-3N | 1+20 | 1+65 | P-209MR | 7.7 | 7.1 | 4.9 |
| LFC-3S | 1+20 | 1+65 | P-209MR | 7.7 | 6.9 | 4.4 |
| LFS-4N | 1+80 | 2+25 | P-307MR | 7.8 | 5.5 | 5.4 |
| LFC-4S | 1+80 | 2+25 | P-209MR | 7.8 | 6.9 | 6.0 |
| LFC-5N | 2+40 | 2+85 | P-209MR | 6.0 | 4.7 | 4.3 |
| LFC-5S | 2+40 | 2+85 | P-209MR | 6.1 | 4.7 | 5.0 |

Even though inconsistency in thickness distributions was observed to some extent, which also exhibited relatively high thickness deviation from the as-built thickness, any relative change in layer thickness is expected to be captured during the CC9 traffic test. Therefore, the full-width GPR survey using this antenna is recommended to conduct at weekly basis, where these profiles can be adopted as ‘Baseline Measurement’ to monitor any possible occurrence of permanent deformation in P-401MR and underlying layers.

## 2 GHz VAN-MOUNTED ANTENNA

As mentioned earlier, 900 MHz antenna was not able to capture P-401MR thickness change between LFS/C-4 and LFC-5 during trial testing, which was later supported by the observations from the baseline GPR data. Full-length GPR testing was conducted with 2 GHz antenna to address this issue. In the data analysis, thicknesses of both P-401MR and the base layer, i.e., P-403MR, P-209, and P-307, were determined. The discussion herein is limited to the distribution of P-401MR thickness, while the distributions of lower layer thickness were included in APPENDIX D.

Figure 27(a) and (b) show the full-length distributions of P-401MR thickness for LFS-1N and -1S respectively. It is observed that the distributions along varying offsets were consistent for both test items. The mean P-401MR thicknesses were 4.5 and 4.1 inches for LFS-1N and -1S respectively, which were close to the as-built thicknesses (i.e., 4.9 and 4.4 for LFS-1N and -1S respectively).

(a)							(b)

Figure 27. P-401MR Thickness in LFS-1N/1S: (a) LFS-1N, and (b) LFS-1S.

Figure 28(a) and (b) show full-length distributions of P-401MR thickness for LFS-2N and -2S respectively. Like LFS-1N and -1S, the distributions along varying offsets were also consistent for both test items. Both mean P-401MR thicknesses were 4.2 inches, which were close to the as-built thicknesses (i.e., 4.4 for both LFS-2N and -2S).

(a)							(b)

Figure 28. P-401MR Thickness in LFS-2N/2S: (a) LFS-2N, and (b) LFS-2S.

Figure 29(a) and (b) show full-length distributions of P-401MR thickness for LFC-3N and -3S respectively. A few locations were excluded from the analysis, which explains the missing data points on the figures. The mean P-401MR thicknesses were 5.0 and 5.3 inches for LFC-3N and -3S respectively and these were close to the as-built thicknesses of 5.1 and 5.2 inches for LFC-3N and -3S respectively.

(a)							(b)

Figure 29. P-401MR Thickness in LFC-3N/3S: (a) LFC-3N, and (b) LFC-3S.

Figure 30(a) and (b) show full-length distributions of P-401MR thickness for LFS-4N and LFC-4S respectively. Several locations were excluded from the analysis and reflected the data gap in the figures. The mean P-401MR thicknesses were 4.9 and 5.4 inches for LFS-4N and LFC-4S respectively and these were close to the as-built thicknesses, i.e., 5.1 and 5.2 inches for LFC-4N and -4S respectively.

(a)							(b)

Figure 30. P-401MR Thickness in LFS/LFC-4N/4S: (a) LFS-4N, and (b) LFC-4S.

Figure 31(a) and (b) show full-length distributions of P-401MR thickness for LFC-5N and -5S respectively. Unlike the previous test items, more discontinuities and/or poor contrasts were observed on the GPR images, which was most likely due to the noise from the embedded instrumentation and conduit and thereby, several locations along multiple offsets were excluded from the analysis. In addition, the thickness distributions were not very consistent. The mean P-401MR thicknesses were close to the as-built thicknesses as reported in Table 4.

(a)							(b)

Figure 31. P-401MR Thickness in LFC-5N/5S: (a) LFC-5N, and (b) LFC-5S.

Table 4. Summary of P-401MR Thickness (2 GHz Antenna)

| Test Item | Start Station | End Station | As-built Thickness, inch | Interpreted Thickness, inch |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | Mean | COV (%) |
| LFS-1N | 0+00 | 0+45 | 4.9 | 4.5 | 4.5 |
| LFS-1S | 0+00 | 0+45 | 4.4 | 4.1 | 4.3 |
| LFS-2N | 0+60 | 1+05 | 4.4 | 4.2 | 4.3 |
| LFS-2S | 0+60 | 1+05 | 4.4 | 4.2 | 5.1 |
| LFC-3N | 1+20 | 1+65 | 5.1 | 5.0 | 5.1 |
| LFC-3S | 1+20 | 1+65 | 5.2 | 5.3 | 4.6 |
| LFS-4N | 1+80 | 2+25 | 5.1 | 4.9 | 2.6 |
| LFC-4S | 1+80 | 2+25 | 5.2 | 5.4 | 4.2 |
| LFC-5N | 2+40 | 2+85 | 3.3 | 3.7 | 8.5 |
| LFC-5S | 2+40 | 2+85 | 3.3 | 3.9 | 9.4 |

In summary, the full-length GPR survey by 2 GHz antenna captured the thickness variation in P-401MR layer. The thickness distributions within the test items were fairly consistent and close to the as-built thickness, which can serve as ‘Baseline Measurement’ to monitor any possible permanent deformation during CC9 traffic test. Full-length GPR survey using 2 GHz is recommended when permanent deformation is observed on the pavement surface.

## 400 MHz VAN-MOUNTED ANTENNA

Full-length thickness distributions of subbase, i.e., P-209MR for LFS-1 through LFS-2, and P-154MR for LFC-3 through LFC-5, were generated based on the analysis of 400 MHz antenna data. Figure 32(a) and (b) show the full-length distributions of P-209MR thickness for LFS-1N and -1S respectively. The thickness distributions were consistent, and the mean thicknesses were close to the as-built thicknesses (as reported in Table 5).

(a)							(b)

Figure 32. P-401MR Thickness in LFS-1N/1S: (a) LFS-1N, and (b) LFS-1S.

Figure 33(a) and (b) show full-length distributions of P-209MR thickness for LFS-2N and -2S respectively. Like LFS-1N and -1S, the thickness distributions were consistent. The mean interpreted thicknesses were close to the as-built thicknesses (as reported in Table 5).

(a)							(b)

Figure 33. P-401MR Thickness in LFS-2N/2S: (a) LFS-2N, and (b) LFS-2S.

Figure 34(a) and (b) show full-length distributions of P-154MR thickness for LFC-3N and -3S respectively. The thickness distribution for LFC-3N was consistent; however, notable inconsistency, followed by missing data points were observed for LFC-3S. It was attributed to the discontinuity in the layer interfaces and poor contrast in the image that prevented to track the bottom of P-154MR accurately. As reported in Table 5, the mean interpreted thicknesses were close to the as-built thicknesses.

(a)							(b)

Figure 34. P-154MR Thickness in LFC-3N/3S: (a) LFC-3N, and (b) LFC-3S.

Figure 35(a) and (b) show ]full-length distributions of P-154MR thickness for LFS-4N and LFC-4S respectively. Thickness distributions of both were fairly consistent. As reported in Table 5, the mean interpreted thicknesses were close to the as-built thicknesses.

(a)							(b)

Figure 35. P-154MR Thickness in LFS/LFC-4N/4S: (a) LFS-4N, and (b) LFC-4S.

Figure 35(a) and (b) show full-length distributions of P-154MR thickness for LFC-5N and LFC-5S respectively. Thickness distributions of both were fairly consistent. As reported in Table 5, the mean interpreted thicknesses were close to the as-built thicknesses.

(a)							(b)

Figure 36. P-154MR Thickness in LFC-5N/5S: (a) LFC-5N, and (b) LFC-5S.

Table 5. Summary of P-209MR/P-154MR Thickness (400 MHz Antenna)

| Test Item | Start Station | End Station | Layer | As-built Thickness, inch | Interpreted Thickness, inch |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Mean | COV (%) |
| LFS-1N | 0+00 | 0+45 | P-209MR | 25.8 | 26.0 | 2.4 |
| LFS-1S | 0+00 | 0+45 | P-209MR | 26.1 | 25.8 | 1.8 |
| LFS-2N | 0+60 | 1+05 | P-209MR | 30.1 | 29.6 | 2.4 |
| LFS-2S | 0+60 | 1+05 | P-209MR | 30.0 | 30.7 | 1.9 |
| LFC-3N | 1+20 | 1+65 | P-154MR | 29.1 | 30.0 | 2.7 |
| LFC-3S | 1+20 | 1+65 | P-154MR | 29.1 | 28.3 | 3.8 |
| LFS-4N | 1+80 | 2+25 | P-154MR | 29.2 | 29.4 | 1.6 |
| LFC-4S | 1+80 | 2+25 | P-154MR | 29.1 | 28.8 | 2.9 |
| LFC-5N | 2+40 | 2+85 | P-154MR | 20.3 | 20.0 | 3.2 |
| LFC-5S | 2+40 | 2+85 | P-154MR | 19.7 | 20.1 | 3.2 |

In summary, layer interface atop P-152MR was captured by 400 MHz antenna and then, subbase thickness was determined. Overall, full-length distributions of subbase thickness were fairly consistent and close to the as-built thickness, which can serve as ‘Baseline Measurement’ to capture any possible permanent deformation during CC9 traffic test. Full-length GPR survey is recommended to conduct using 400 MHz antenna, if permanent deformation: (a) observed on the pavement surface, and (b) indicated in coil sensor responses.

# SUMMARY and recommendations

Summary

- Full-width survey along transverse direction was conducted using 900 MHz cart-mounted GPR antenna at the selected stations on all test items. After post-processing of GPR image and data analysis, transverse thickness profiles of both P-401MR and underlying layers at shallow depth (i.e., P-403MR in LFS-1 through LFS-2, P-209MR in LFC-3 through LFS-5, and P-307MR in LFS-4N) were generated. These profiles will serve as ‘Baseline Measurement’ to monitor any possible occurrence of permanent deformation in P-401MR and the underlying layers during CC9 traffic test.

- Full-length survey was conducted by 2 GHz van-mounted GPR antenna that captured the thickness variation in P-401MR layer in LFC-5N/5S. In addition, P-401MR thickness distributions within each test item were fairly consistent and close to the as-built thickness, which can be adopted as an additional ‘Baseline Measurement’ to monitor any possible permanent deformation in P-401MR layer during CC9 traffic test.

- Full-length survey was also conducted by 400 MHz van-mounted GPR antenna that captured the layer interface atop P-152MR. Subsequent interpretation of subbase thickness can be adopted as ‘Baseline Measurement’ to monitor any possible permanent deformation in the subbase during CC9 traffic test.

Recommendations

- Full-width GPR survey using 900 MHz antenna is recommended for weekly testing, and monitor possible occurrence of permanent deformation in P-401MR and underlying layers at shallow depth.

- Full-length GPR survey using the 2 GHz antenna is recommended to monitor permanent deformation in P-401MR layer, specially LFS-5N/5S, when permanent deformation is observed on the surface.

- Full-length GPR survey using the 400 MHz antenna is recommended to monitor permanent deformation in the subbase, if permanent deformation: (a) observed on the pavement surface, and (b) indicated in coil sensor responses.

# REFERENCES

Saarenketo, T., and Scullion, T. (1999). Road Evaluation with Ground Penetrating Radar. Journal of Applied Geophysics, 43, 119-138.

Al-Qadi, I. L., Lahouar, S., and Loulizi, A. (2003). Successful Application of GPR for Quality Assurance/Quality Control of New Pavements. Proceedings of Transportation Research Board (TRB), Washington, DC.

Ahmed, M. U., Tarefder, R. A., and Maji, A. K. (2016). Incorporating transmitter–receiver offset to interpret pavement layer thicknesses by GPR. Case Studies in Nondestructive Testing and Evaluation, Elsevier, 6(A), 94-104.

Cao, Y., Dai, S., Labuz, J. F., and Pantelis, J. (2007). Implementation of Ground Penetrating Radar. Report No. MN/RC 2007-34, Minnesota Department of Transportation, MN, USA.

GSSI. (2003). SIR 3000 Manual. Geophysical Survey Systems, Inc., NH, USA.

GSSI. (2011a). SIR 30 Manual. Geophysical Survey Systems, Inc., NH, USA.

Tarefder, R. A., and Ahmed, M. U. (2016). Optimal Use of Falling Weight Deflectometer and Ground Penetrating Radar. Report No. NM12SP-01, University of New Mexico, Albuquerque, NM, USA. <https://dot.state.nm.us/content/dam/nmdot/Research/Final_report-GPR.pdf>

GDIT. (2020). Construction Cycle 9 As-Built Drawings. National Airport Pavement Testing Facility, NJ, USA.

GSSI. (2011b). RADAN 7 Manual. Geophysical Survey Systems, Inc., NH, USA.

Horizon Engineering Consulting LLC (HEC). (2020). Preparation and Recommendations for CC9 Baseline GPR Survey. Task Order (TO) 3, Deliverable 5.1.63, National Airport Pavement Testing Facility, NJ, USA

Edwards, L., and Mason, Q. (2011). Evaluation of Nondestructive Methods for Determining Pavement Thickness. Report No. ERDC/GSL TR-11-41, US Army Corps of Engineers, Vicksburg, MS, USA.

APPENDIX A – Distribution of 2-Way Travel Time (900 MHz Antenna)

(a)							(b)

(c)							(d)

Figure A1. 2-way travel time in LFS-1N/1S: (a) LFS-1N (STA: 0+15), (b) LFS-1S (STA: 0+15), (c) LFS-1N (STA: 0+30), and (d) LFS-1S (STA: 0+30).

(a)							(b)

(c)							(d)

Figure A2. 2-way travel time in LFS-2N/2S: (a) LFS-2N (STA: 0+15), (b) LFS-2S (STA: 0+15), (c) LFS-2N (STA: 0+30), and (d) LFS-2S (STA: 0+30).

(a)							(b)

(c)							(d)

Figure A3. 2-way travel time in LFC-3N/3S: (a) LFC-3N (STA: 0+15), (b) LFC-3S (STA: 0+15), (c) LFC-3N (STA: 0+30), and (d) LFC-3S (STA: 0+30).

(a)							(b)

(c)							(d)

Figure A4. 2-way travel time in LFS/C-4N/4S: (a) LFS-4N (STA: 0+15), (b) LFC-4S (STA: 0+15), (c) LFS-4N (STA: 0+30), and (d) LFC-4S (STA: 0+30).

(a)							(b)

(c)							(d)

Figure A5. 2-way travel time in LFC-5N/5S: (a) LFC-5N (STA: 0+15), (b) LFC-5S (STA: 0+15), (c) LFC-5N (STA: 0+30), and (d) LFC-5S (STA: 0+30).

APPENDIX B – Distribution of 2-Way Travel Time (2 GHz Antenna)

(a)							(b)

Figure B1. 2-way travel time in P-401MR (LFS-1N/1S): (a) LFS-1N, and (b) LFS-1S.

(a)							(b)

Figure B2. 2-way travel time in P-401MR (LFS-2N/2S): (a) LFS-2N, and (b) LFS-2S.

(a)							(b)

Figure B3. 2-way travel time in P-401MR (LFC-3N/3S): (a) LFC-3N, and (b) LFC-3S.

(a)							(b)

Figure B4. 2-way travel time in P-401MR (LFS/C-4N/4S): (a) LFS-4N, and (b) LFC-4S.

(a)							(b)

Figure B5. 2-way travel time in P-401MR (LFC-5N/5S): (a) LFC-5N, and (b) LFC-5S.

(a)							(b)

Figure B6. 2-way travel time in P-403MR (LFS-1N/1S): (a) LFS-1N, and (b) LFS-1S.

(a)							(b)

Figure B7. 2-way travel time in P-403MR (LFS-2N/2S): (a) LFS-2N, and (b) LFS-2S.

(a)							(b)

Figure B8. 2-way travel time in P-209MR (LFC-3N/3S): (a) LFC-3N, and (b) LFC-3S.

(a)							(b)

Figure B9. 2-way travel time in P-307MR/209MR (LFS/C-4N/4S): (a) LFS-4N, and (b) LFC-4S.

(a)							(b)

Figure B10. 2-way travel time in P-307MR/P-209MR (LFS/C-4N/4S): (a) LFS-4N, and (b) LFC-4S.

APPENDIX C – Distribution of 2-Way Travel Time (400 MHz Antenna)

(a)							(b)

Figure C1. 2-way travel time in P-209MR (LFS-1N/1S): (a) LFS-1N, and (b) LFS-1S.

(a)							(b)

Figure C2. 2-way travel time in P-209MR (LFS-2N/2S): (a) LFS-2N, and (b) LFS-2S.

(a)							(b)

Figure C3. 2-way travel time in P-154MR (LFC-3N/3S): (a) LFC-3N, and (b) LFC-3S.

(a)							(b)

Figure C4. 2-way travel time in P-154MR (LFS/C-4N/4S): (a) LFS-4N, and (b) LFC-4S.

(a)							(b)

Figure C5. 2-way travel time in P-154MR (LFC-5N/5S): (a) LFC-5N, and (b) LFC-5S.

APPENDIX D – DISTRIBUTION OF P-403MR/P-209MR/P-307MR THICKNESS (2 GHz ANTENNA)

(a)							(b)

Figure D1. P-403MR Thickness in LFS-1N/1S: (a) LFS-1N, and (b) LFS-1S.

(a)							(b)

Figure D2. P-403MR Thickness in LFS-2N/2S: (a) LFS-2N, and (b) LFS-2S.

(a)							(b)

Figure D3. P-209MR Thickness in LFC-3N/3S: (a) LFC-3N, and (b) LFC-3S.

(a)							(b)

Figure D4. P-209MR Thickness in LFS/LFC-4N/4S: (a) LFS-4N, and (b) LFC-4S.

(a)							(b)

Figure D5. P-209MR Thickness in LFC-5N/5S: (a) LFC-5N, and (b) LFC-5S.