Date – March 8, 2021

Test - ASTM E1703 – Rut Depth of Pavement Surface.

Equipment – 16ft Straight Edge

Fully Extended Gauge Length – 1.05

Technicians - H. Fermin , J. Alcoba, J Landy Jr

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| Station | Side of Test Section | Centerline of Test Location | Location - -12.75 / -17.25 | Location -10’ / -19’ |
|  |  |  | Rut Depth | Rut Depth |
| Time | 11:05 AM |  |  |  |
| Station 2+55 | North | -15'-0" / .095 | .076 / .188 | .104 / .115 |
| Station 2+70 | North | -15'-0" / .116 | .116 / .185 | .0435 / .153 |
| Time | 11:20 AM |  |  |  |
| Station 2+55 | North | -15'-0" / .0795 | 0.071 / .183 | .110 / .134 |
| Station 2+70 | North | -15'-0" .171 | .139 / .195 | .040 / .084 |
| Time | 11; 35 AM |  |  |  |
| Station 2+55 | North | -15'-0" / .083 | .062 / .224 | .118 / .149 |
| Station 2+70 | North | -15'-0" / .133 | .103 / .228 | .052 / .181 |